Prepare Glass Milk from Silicon Dioxide

- Use SiO₂ powder, 325 mesh; one published protocol uses Sigma 342890.

- Suspend 21 g SiO₂ in 40 mL of 10% HCl in a polypropylene 50-mL tube.

- Mix/roll for 4 h.

- Centrifuge at 2,000 × g for 5 min and carefully remove the acid.

- Resuspend the pellet in 40 mL DI/Milli-Q water, centrifuge again at 2,000 × g for 5 min, and remove the supernatant.

- Repeat the water wash six times total, fully resuspending the silica each time.

- Check the final wash; the supernatant should be approximately pH 7–8. Continue washing if it remains acidic.

- After removing the final wash, resuspend the silica to a final volume of 30 mL with nuclease-free or Milli-Q water.

Approximately 700 mg/mL SiO₂ glass milk.

Mix thoroughly before use because the silica settles rapidly.